## Slide 3: Outline
Review Material Properties
Band gap
Absorption Coefficient
Mobility

## Slide 33
Properties | Si | Ge | GaAs
Atoms/cm3 | 5.0 x 1022 | 4.42 x 1022 | 4.42 x 1022
Atomic Weight | 28.09 | 72.60 | 144.63
Breakdown Field | approx. 3 x 105 | approx. 1 x 105 | approx. 4 x 105
Crystal Structure | Diamond | Diamond | Zincblende
Density (g/cm3) | 2.328 | 5.3267 | 5.32
Dielectric Constant | 11.9 | 16.0 | 13.1
Effective Density of States in the Conduction Band, Nc (cm-3) | 2.8 x 1019 | 1.04 x 1019 | 4.7 x 1017
Effective Density of States in the Valence Band, Nv (cm-3) | 1.04 x 1019 | 6.0 x 1018 | 7.0 x 1018
Electron Affinity (V) | 4.05 | 4.0 | 4.07
Energy Gap at 300K (eV) | 1.12 | 0.66 | 1.424
Intrinsic Carrier Concentration (cm-3) | 1.45 x 1010 | 2.4 x 1013 | 1.79 x 106
Intrinsic Debye Length (microns) | 24 | 0.68 | 2250
Intrinsic Resistivity (ohm-cm) | 2.3 x 105 | 47 | 108
Lattice Constant (angstroms) | 5.43095 | 5.64613 | 5.6533
Linear Coefficient of Thermal Expansion, ΔL/L/ΔT (1/deg C) | 2.6 x 10-6 | 5.8 x 10-6 | 6.86 x 10-6
Melting Point (deg C) | 1415 | 937 | 1238
Minority Carrier Lifetime (s) | 2.5 x 10-3 | approx. 10-3 | approx. 10-8
Mobility (Drift) (cm2/V-s) µn, electrons | 1500 | 3900 | 8500
Mobility (Drift) (cm2/V-s) µp, holes | 475 | 1900 | 400
Optical Phonon Energy (eV) | 0.063 | 0.037 | 0.035
Phonon Mean Free Path (angstroms) | 76 (electron) 55 (hole) | 105 | 58
Specific Heat (J/g-deg C) | 0.7 | 0.31 | 0.35
Thermal Conductivity at 300 K (W/cm-degC) | 1.5 | 0.6 | 0.46
Thermal Diffusivity (cm2/sec) | 0.9 | 0.36 | 0.24
Vapor Pressure (Pa) | 1 at 1650 deg C; 10-6 at 900 deg C | 1 at 1330 deg C; 10-6 at 760 deg C | 100 at 1050 deg C; 1 at 900 deg C