## Slide 1: Theory of the P-N junction

## Slide 2: Generation and Recombination
4.1 Semiconductor transport equations

## Slide 3: Continuity equation

## Slide 4: 4.2 Generation & Recombination
Thermal Generation & Recombination

## Slide 5: 4.3 Transition Rates
4.3.1 fermi’s golden rule
Matrix element coupling initial and final states

## Slide 6: Derivation of Fermi’s golden rule

## Slide 8: 4.3.2 optical processes in a two level system

## Slide 9: Steady state

## Slide 10: 4.4 photon generation

## Slide 11: 4.4.3 microscopic description of absorption
Dipole approximation

## Slide 14: Direct gap

## Slide 15: Indirect band gap

## Slide 16: 4.4.6 other types of behavior
Multiple step photon generation
Absorptions by excitons and sensitisers

## Slide 17: 4.5 Recombination

## Slide 18: 4.5.2 Radiative recombination
Derivation of the radiative recombination rate
Intial state：
Final state：

## Slide 21
By last session’s conclusion
Substituting for

## Slide 22
For application, interested in one direction, reduce to 1/4

## Slide 25: 4.5.3 simplified expressions for radiative recombination
Carrier density independent and properties of the material

## Slide 26
Degenerate semiconductor
Minority carrier radiative lifetime

## Slide 27
Larger for materials with a high absorption coefficient, and therefore radiative recombination
is more important
in direct bad gap
materials.
Relative to absorption, contributions from energy levels closer to the band edges are really important

## Slide 28
When =qV
Radiative recombination from either band to impurity states inside the band gap can be very important, and can dominate over band-to band events.

## Slide 30: 4.3 bimolecular recombination

## Slide 31: MULTI-STEP PROCESS?
Relaships between rates and carrier densities?

## Slide 32: Three carrier –process : Auger recombination

## Slide 34: Lifetime for Auger recombination
In p-type material

## Slide 35: Momentum concervation

## Slide 36: Shockley Read Hall recombination

## Slide 37: Derivation of SRH recombination rate

## Slide 42: Surface and grain boundary Recombination

## Slide 45: Traps vs recombination centers

## Slide 46: Chapter 3 Electrons& Holes

## Slide 47: Quasi thermal equilibrium

## Slide 48: Current densities under bias

## Slide 54: P-n junction
http://www.acsu.buffalo.edu/~wie/applet/pnformation/pnformation.html

## Slide 56: Depletion region

## Slide 57: 6.4 carrier and current densities

## Slide 58: B.C:boundary condition

## Slide 61: Currents and carrier density in the SPACE CHARGE REGION

## Slide 62: TOTAL CURRENT DENSITY

## Slide 63: General solution

## Slide 64: Jn

## Slide 65: Jp

## Slide 66: Jscr

## Slide 67: P-N JUNCTION
DARK
UNDER ILLUMINATION
characteristics

## Slide 68: Dark
Equilibrium 0
Under applied bias

## Slide 73: Under Illumination
Short circuit V=0

## Slide 75: QE in special cases
Thick-neutral layers are much thicker than diffusion length

## Slide 76
If Sn=Sp=0 q times the flux of photons absorbed that layer

## Slide 81: P-n junction as a photovoltaic cell

## Slide 83: Effects on p-n junction Characteristics